Appendix

Registered Trademark and Packaging Standard of Steel Rebar of the Shanghai Futures Exchange

|  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Serial  No. | Registered Enterprise | Registration Date | Place of Origin | Trademark | Designation | Diameter (mm) | Length (m) | Piece/  Bundle | Bundle Weight (kg) | Bundle/  Lot |
| 36 | Shandong Laigang Yongfeng Steel Corp. | June 2014 | Dezhou,  Shandong | Yongfeng | HRB400 | 16 | 9 | 224 | 3185 | 94 |
| 12 | 160 | 3034 | 99 |
| 18 | 9 | 178 | 3204 | 94 |
| 12 | 140 | 3360 | 89 |
| 20 | 9 | 144 | 3201 | 94 |
| 12 | 108 | 3201 | 94 |
| 22 | 9 | 122 | 3272 | 92 |
| 12 | 84 | 3004 | 100 |
| 25 | 9 | 85 | 2945 | 102 |
| 12 | 70 | 3234 | 93 |
|  |  |  |  |  |  |  |  |  |  |  |

Note:

1. The “bundle weight” in the table is theoretical value and the “bundle/lot” is theoretical calculation value. Both are for reference only;

2. For the warrant weight, the actual weight is taken as final.