**Appendix 1**

**Revisions to the *Copper Cathode Contract Specifications***

Note: Double strikethroughs indicate deletion and red and bold indicate new addition

|  |  |
| --- | --- |
| **Revised Version** | **Version on August 18, 2020** |
| **Grade and Quality Specifications：**  Standard: #1 Standard copper (Cu-CATH-2) as prescribed in the National Standard GB/T 467-2010, with total copper and silver content not less than 99.95%.  Substitute: Grade A copper (Cu-CATH-1) as prescribed in National Standard GB/T 467-2010; or Grade A copper (Cu-CATH-1) as prescribed in BS EN 1978:1998. | **Grade and Quality Specifications：**  Standard: #1 Standard copper (Cu-CATH-2) as prescribed in the National Standard GB/T 467-2010, with total copper and silver content not less than 99.95%.  Substitute: Grade A copper (Cu-CATH-1) as prescribed in National Standard GB/T 467-2010; or Grade A copper (Cu-CATH-1) as prescribed in BS EN 1978:1998. |
| **II. Quality specifications**  (1) Subject to all specifications on standard copper cathode, the primary component of copper and silver shall not be less than 99.95%. Grade A copper (Cu-CATH-1) as prescribed in National Standard GB/T 467-2010 or Grade A copper (Cu-CATH-1) as prescribed in BS EN 1978:1998. | **II. Quality specifications**  (1) Subject to all specifications on standard copper cathode, the primary component of copper and silver shall not be less than 99.95%. |
| **III. The Exchange approved manufacturers and registered brands**  Copper cathode used for physical delivery must be of the brand registered with the Exchange. Delivery of high purity copper cathode is replaceable. The specific registered brand as well as the premium and discount standard will be provided and announced by the Exchange. | **III. The Exchange approved manufacturers and registered brands**  Copper cathode used for physical delivery must be of the brand registered with the Exchange. Delivery of high purity copper cathode is replaceable. The specific registered brand as well as the premium and discount standard will be provided and announced by the Exchange. |